Tertiary Infotech Academy Pte Ltd

UEN: 201200696W

LEARNER GUIDE

For

Mastering Semiconductor Key Modules for Enhanced CMOS Process Integration and Device Performance

TGS Ref No: TGS-2024051248

Conducted by

Tertiary Infotech Academy Pte Ltd

UEN: 201200696W

Version 9.0

# DOCUMENT VERSION CONTROL RECORD

| Version Number | Effective Date of Release | Summary of Included Changes | Author |
| --- | --- | --- | --- |
| 8.0 | 20 August 2026 | Complete v7 coverage baseline, eight activities and aligned Learner Guide. | Dr Alfred Ang |
| 9.0 | 20 August 2026 | Re-aligned to the 139-slide Mobile Photography design-system rebuild, four learning blocks and regenerated activity slide map. | Dr Alfred Ang |

# TABLE OF CONTENTS

Right-click and update field in Word if page numbers are not shown.

# How to Use This Guide

This guide holds the detailed procedures intentionally omitted from the concept-led slide deck. Work through the eight activities in sequence, keep evidence in the named folder, and use acceptance criteria before moving to the next integration decision.

| Field | Details |
| --- | --- |
| Course | Mastering Semiconductor Key Modules for Enhanced CMOS Process Integration and Device Performance |
| Course code | TGS-2024051248 |
| TSC | Process Integration · ELE-SIS-4002-1.1 |
| Duration | 16 hours over 2 days |
| Assessment | Written Assessment (WA-SAQ) - 2 open-ended questions, K1-K2, 1 hour, open book. Practical Performance (PP) - 2 open-ended tasks, A1-A5, 1 hour, open book. |
| LMS | https://lms-tms.tertiaryinfotech.com/ |

# Learning and Assessment Alignment

LO1: Identify process flows and modules for specific CMOS technologies in manufacturing.

LO2: Determine CMOS device performance and verify process integration in accordance with product specifications.

## Knowledge and Ability Criteria

K1: Specific technology process flow

K2: Types of performance metrics

A1: Identify process flow for the specific technology in the manufacturing process in accordance with technology specifications

A2: Determine process interaction between and within process modules to the specific technology in accordance with technology specifications

A3: Determine device performance in accordance with product specifications

A4: Verify process integration performance to the specific technology in accordance with product specifications

A5: Determine follow-up actions required

# Before You Start - What You Need

The current v9.0 learner slides and this Learner Guide.

The complete activities/ folder with Markdown/PDF resources and Excel workbooks.

Microsoft Excel or compatible spreadsheet software with automatic calculation enabled.

A drawing tool or A3 paper for process maps and integration diagrams.

Access to the LMS for courseware download and assessment submission.

# Topic 1 - CMOS Process Modules and Process Flow

## Learning Block 1A - Patterning, Etch and Fab Control

Build reliable patterns while controlling contamination, CD, overlay and profile.

### The Wafer Fab as a System

Product flow: hundreds of tightly coupled operations

Cleanroom: particles and molecular contamination are controlled

Integration: each module owns incoming and outgoing evidence

Release logic: a pass is a measured decision, not an assumption

### Contamination Has Multiple Pathways

Particles: block patterns and create opens or shorts

Ions: shift electrical behaviour and junction properties

Organics: interfere with adhesion, exposure and interfaces

Water and tools: transport hidden contamination between modules

### The Lithography Stack

Mask or reticle carries the intended geometry

Resist converts optical energy into a soluble contrast

Alignment connects the current level to prior levels

Developed resist becomes the etch or implant mask

### Mask Tone and Resist Tone

Clear-field and dark-field masks invert where light passes

Positive resist removes exposed regions

Negative resist retains exposed regions

The combination determines whether a hole or island remains

### Resist Coating and Bake

Prime improves adhesion on the prepared surface

Spin speed and dispense control resist thickness

Soft bake removes solvent without damaging image response

Edge bead and coverage affect focus and defectivity

### Resolution, NA and Process Margin

Wavelength: shorter light supports smaller features

Numerical aperture: higher NA improves resolution

Depth of focus: normally shrinks as NA rises

Usable window: pitch, resist and variation set margin

### Overlay, OPC and Mask Protection

Overlay error shifts one layer against another

OPC pre-distorts features to counter imaging effects

Antireflective layers reduce standing-wave effects

Pellicles and inspection reduce repeating defects

### Wet Etch versus Dry Etch

Wet etch is often isotropic and can undercut

Plasma/RIE supports directional profiles

Chemistry controls material reaction

Bias, pressure and transport influence sidewalls and damage

### Etch Selectivity and Profile

Selectivity protects resist and stop layers

Over-etch clears residual film but consumes margin

Microloading makes local pattern density matter

Endpoint and cross-section evidence localise failure

### Strip and Clean

Wet strip dissolves resist where surfaces tolerate chemistry

Dry strip removes organics but can damage sensitive layers

RCA-type cleans target particles, organics and metals

Drying must avoid watermarking and recontamination

### Pattern-Transfer Window

Lithography CD sets the incoming geometry

Etch bias changes the final feature

Across-wafer signatures expose non-uniformity

Pre- and post-etch metrology localises the dominant shift

### Patterning Evidence Gate

Geometry: CD, overlay and profile

Defects: bridge, open, pinhole, residue or collapse

Mechanism: exposure, develop, etch or clean

Action: release, conditional release, hold or scrap

## Learning Block 1B - Implant, Thermal, Films and Integrated Flow

Control material modification, film formation, planarity and FEOL-to-BEOL hand-offs.

### Implant Dose and Energy

Dose controls total implanted ions

Energy controls the depth distribution

Tilt and twist reduce channeling and shadowing

Uniform scanning protects within-wafer consistency

### Beamline Risks

Charging can deflect beams or damage dielectrics

Channeling produces unexpectedly deep tails

Mask topography creates shadowed regions

Beam focus and scan strategy affect uniformity

### Crystal Damage and Activation

Implant collisions create vacancies and interstitials

Anneal repairs lattice damage

Activation places dopants on useful sites

Electrical improvement can coexist with diffusion

### Diffusion, Furnace and RTP

Furnace cycles favour batch throughput and long soak

RTP uses fast ramps and short dwell

Thermal budget controls activation and junction movement

The best cycle balances electrical target with geometry

### Thermal Oxidation

Silicon is consumed as silicon dioxide grows

Dry oxidation grows slowly with strong film quality

Wet oxidation grows faster for thicker films

Temperature, time and surface condition control integrity

### CVD, PECVD and Epitaxy

CVD: film forms through surface reactions

PECVD: plasma lowers process temperature

Epitaxy: deposited crystal follows the substrate lattice

Selection: conformality, stress, purity and thermal budget

### PVD, Barrier and Seed

Sputtering transports target atoms to the wafer

Directional coverage challenges deep features

Barrier films limit metal diffusion

Continuous seed enables uniform electrofill

### Copper Dual Damascene

Pattern vias and trenches in dielectric

Deposit liner, barrier and seed

Electrofill copper without seams or voids

Polish overburden while protecting pattern density

### CMP Mechanics and Chemistry

Pad contact and slurry chemistry work together

Downforce, speed and pad state affect removal

Selectivity protects stop layers

Post-CMP clean removes abrasive and metal residue

### Planarity Failure Modes

Dishing removes too much metal in wide features

Erosion lowers dense pattern regions

Incomplete clear leaves conductive residue

Topography and electrical continuity must both pass

### Integrated FEOL and BEOL

Isolation and wells define device regions

Gate and source/drain form transistors

Contacts and interconnect create connectivity

Passivation and wafer sort close wafer fabrication

### Cross-Module Budgeting

Thermal budget accumulates across later steps

Topography changes the next lithography window

Contamination transfers through surfaces and tools

Every hand-off needs evidence and an owner

# Topic 2 - CMOS Process Integration and Performance

## Learning Block 2A - Integration Performance, Yield and Reliability

Use metrology, electrical data and reliability evidence to verify product performance.

### Isolation and Well Integration

LOCOS is simple but creates bird's-beak encroachment

STI supports scaling through etched and filled trenches

Well architecture controls body regions

Stress, CD and topography affect device behaviour

### Transistor Formation

Gate stack sets electrostatic control

Source/drain implants establish junctions

Spacers sequence extension and deep implants

Contacts must preserve silicide and junction integrity

### Yield Is Multiplicative

Wafer-fab yield reflects process survival

Wafer-sort yield reflects functional die

Packaging yield reflects assembly and final test

One stage can erase gains made at another

### Defect Density and Die Area

Larger die expose more area to random defects

Clustered defects violate simple random assumptions

Systematic defects need separate treatment

Yield models support prediction, not proof

### Metrology by Question

Ellipsometry: thin-film thickness and optics

Profilometry/AFM: step height and topography

SEM/TEM: CD, profile and internal structure

SIMS/Auger: concentration and surface composition

### Measurement Strategy

Before and after: isolate the suspected module

Spatial map: expose centre-edge or chamber signatures

Resolution: match instrument to the feature

Correlation: connect physical and electrical evidence

### Electrical Performance

Four-point probe measures sheet resistance

Gate-oxide integrity tests dielectric weakness

I-V curves reveal threshold, leakage and drive

Product specifications decide pass/fail

### Reliability Evidence

Mechanism explains degradation

Accelerated stress creates measurable change

Failure criterion defines the endpoint

Physical confirmation links failure to cause

### HCI, TDDB and Electromigration

Hot carriers damage the channel interface

TDDB accumulates dielectric damage over time

Electromigration moves metal under current density

Geometry, material and temperature change lifetime

### Control Limits versus Specifications

Control limits describe process behaviour

Specification limits describe product requirements

A stable process may still be off target

An in-spec point can signal a process shift

### Capability: Cp and Cpk

Cp compares specification width with spread

Cpk also reflects centering

Capability follows stability assessment

Use the approved threshold and risk context

### Evidence-Based Release

Define the product requirement

Select physical and electrical evidence

Compare with limits and uncertainty

Document disposition and follow-up

## Learning Block 2B - SPC, Packaging and Future Integration

Control excursions, close the feedback loop and evaluate next-generation choices.

### SPC as a Feedback System

Sample the process with a rational subgroup

Plot performance against behaviour-based limits

Detect special-cause signals

Contain risk and restore control with evidence

### Select the Chart from the Data

Variable data: measurements such as CD

Attribute data: counts or proportions

Subgroup size decides Xbar-R versus Xbar-S

Opportunity and sample size decide p, np, c or u

### Variable Control Charts

Xbar tracks subgroup centre

R or S tracks within-subgroup spread

The two charts answer different questions

A mean chart is incomplete without spread

### Attribute Control Charts

p chart: proportion defective, variable sample size

np chart: defective count, constant sample size

c chart: defect count, constant opportunity

u chart: defects per unit, variable opportunity

### Signals Beyond One Point

A point beyond a limit is a strong signal

Runs and trends expose non-random change

Stratification reveals tool, wafer or time source

Rules must be defined before interpretation

### Excursion Response

Contain: hold material and preserve evidence

Stratify: tool, chamber, wafer, product and time

Correct: controlled change with rollback criteria

Verify: stable behaviour and capability

### Packaging Process Flow

Prepare and thin wafer

Separate, inspect and attach die

Create electrical interconnect

Seal, plate, final-test and burn-in as required

### Wire Bond and Flip Chip

Wire bond is flexible but adds loop length

Flip chip raises I/O density

Underfill and joint quality manage mechanical risk

Inspection and test protect assembly yield

### 2.5D, 3D and Chiplets

Interposers connect multiple dies

3D stacks use vertical connections

Known-good-die and thermal design are inputs

Integration control crosses organisations

### FinFET

A fin raises the channel above substrate

Multiple gate surfaces improve control

Fin geometry and parasitics affect performance

Patterning and variability challenge manufacturing

### GAAFET Nanosheets

Gate surrounds the channel

Stacked sheets increase effective width

Release, inner spacer and contacts are critical

Metrology must resolve buried geometry

### Beyond Today's CMOS

Vertical transistors change current direction

2D materials offer ultrathin channels

Quantum devices require cryogenic control

Every concept still needs capability and reliability gates

# Detailed Step-by-Step Activities

## Activity 1 - Build a CMOS Process Module Map

| Field | Details |
| --- | --- |
| Goal | Organise the legacy module coverage into a defensible FEOL-to-BEOL flow and expose the interfaces that can propagate variation. |
| Scenario | A new 300 mm logic product is moving from process development into a pilot manufacturing line. The integration team needs one agreed process map before module owners set recipes and control plans. |
| Alignment | LO1 · K1, A1, A2 |
| Duration | 45 minutes |
| Folder | activities/activity-01-process-module-map/ |

### What You Need

Activity worksheet and evidence template in this folder

Learner slides covering wafer fab, photolithography, etch, implant, thermal, film, CMP and integrated flows

A3 paper or a digital drawing tool

### Step-by-Step

- Open the worksheet and write the target product assumptions: substrate type, logic technology family and the intended final device outcome.

- Create seven module lanes: photolithography, etch/clean, ion implantation, diffusion/RTP, film deposition, CMP and metrology/control.

- Place the major FEOL stages in order: wafer preparation, isolation, well formation, gate stack, source/drain formation and contacts.

- Add the BEOL stages: dielectric deposition, via/trench patterning, barrier/seed, metal fill, CMP, passivation and wafer sort.

- For each hand-off, identify the incoming measurable characteristic, such as CD, overlay, film thickness, dose, sheet resistance or surface planarity.

- Mark at least three feedback loops where metrology can cause hold, rework, recipe correction or engineering disposition.

- Circle two interactions where a change in one module can create a downstream electrical or yield effect.

- Check the map against the provided process-flow slides and correct missing or duplicated stages.

- Export or photograph the final map and name the evidence file A01-process-map.

### Acceptance Criteria

[ ] The map contains all seven key process modules and distinguishes FEOL from BEOL.

[ ] At least eight process hand-offs have a measurable characteristic.

[ ] At least three control/feedback loops and two cross-module interactions are justified.

### Reflection and Evidence

Which module has the greatest ability to propagate a hidden defect downstream, and why?

What evidence would allow the integration owner to release the lot to the next module?

Save the completed evidence with the A01- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

## Activity 2 - Diagnose a Pattern-Transfer Process Window

| Field | Details |
| --- | --- |
| Goal | Connect mask/resist/exposure decisions to etch profile and select a stable corrective action without masking the root cause. |
| Scenario | A contact layer shows intermittent bridging and open defects. Lithography CD, resist profile and plasma-etch selectivity must be reviewed together rather than as isolated module results. |
| Alignment | LO1 · K1, A2 |
| Duration | 60 minutes |
| Folder | activities/activity-02-pattern-transfer-window/ |

### What You Need

Pattern-transfer worksheet and process-window workbook

Legacy diagrams on resist polarity, Rayleigh resolution, OPC, selectivity and anisotropy

Calculator or spreadsheet software

### Step-by-Step

- Review the defect images in the worksheet and classify each as bridge, open, incomplete etch, undercut or resist-collapse risk.

- Open pattern-transfer-window.xlsx and read the focus, exposure dose, post-develop CD and post-etch CD observations.

- Mark cells that violate the target post-etch CD range of 88-112 nm.

- Compare the lithography CD bias with the post-etch CD bias to decide whether the dominant shift occurs before or during etch.

- Check whether edge cells fail more often than centre cells; record the spatial signature.

- Select one lithography lever (focus, dose, resist thickness or bake) and one etch lever (gas ratio, bias power, pressure or over-etch).

- Predict the intended effect and one possible side effect for each lever.

- Write a confirmation plan using CD-SEM before etch, CD-SEM after etch and profile inspection on a cross-section.

- Record a release decision: accept, conditional release, hold for engineering, or scrap.

### Acceptance Criteria

[ ] Every defect is linked to a plausible lithography/etch mechanism.

[ ] The dominant CD-shift stage is supported by before/after evidence.

[ ] Corrective levers include predicted benefit, risk and verification measurement.

### Reflection and Evidence

Why can improving resolution reduce depth of focus?

When does additional over-etch protect yield, and when does it create reliability risk?

Save the completed evidence with the A02- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

## Activity 3 - Balance Implantation and Thermal Budget

| Field | Details |
| --- | --- |
| Goal | Create an implant-to-anneal decision trail that balances activation, junction depth, damage recovery and channeling risk. |
| Scenario | After a source/drain extension implant, sheet resistance is above target and short-channel control is drifting. The team must distinguish dose/energy error from activation and diffusion effects. |
| Alignment | LO1 · K1, A2, A3 |
| Duration | 60 minutes |
| Folder | activities/activity-03-implant-thermal-budget/ |

### What You Need

Implant and RTP data cards in the worksheet

Legacy diagrams for beam scanning, channeling, damage and RTP

Evidence template

### Step-by-Step

- Read the target dose, implant energy, tilt/twist, sheet resistance and junction-depth specifications.

- Compare actual dose and energy with the target and note whether the deviation can explain the electrical signature.

- Inspect the channeling indicator and decide whether tilt/twist or an amorphising layer should be reviewed.

- Use the damage/activation card to separate as-implanted lattice damage from electrically active dopant.

- Compare the furnace and RTP thermal cycles by peak temperature, dwell time and ramp rate.

- Predict how each thermal cycle affects activation, lateral diffusion and junction depth.

- Choose a containment action for the current lot and a recipe action for the next engineering split.

- Define the minimum verification set: sheet resistance map, SIMS profile or junction-depth proxy, and electrical monitor.

- Complete the risk statement: action, expected benefit, possible adverse effect and stop condition.

### Acceptance Criteria

[ ] The recommendation distinguishes implant dose/energy, damage and activation mechanisms.

[ ] Thermal-budget effects on activation and diffusion are explicit.

[ ] Follow-up measurements can confirm or reject the proposed cause.

### Reflection and Evidence

Why does a shorter high-temperature RTP cycle often protect shallow junctions?

How can a sheet-resistance improvement still hide a device-performance problem?

Save the completed evidence with the A03- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

## Activity 4 - Integrate Film Deposition and CMP

| Field | Details |
| --- | --- |
| Goal | Trace deposition, fill and CMP interactions and design a verification plan that protects both planarity and electrical performance. |
| Scenario | A dual-damascene copper level meets line-resistance targets at wafer centre but fails near the edge with dishing, erosion and suspected barrier continuity loss. |
| Alignment | LO1 · K1, A2, A4 |
| Duration | 60 minutes |
| Folder | activities/activity-04-film-cmp-integration/ |

### What You Need

Cross-section cards and film/CMP worksheet

Legacy diagrams for barrier/seed, copper fill, slurry, polishing and post-CMP clean

Evidence template

### Step-by-Step

- Label the dielectric, barrier/liner, seed, copper fill and overburden layers on the supplied cross-section.

- Identify which layer prevents diffusion and which layer enables electroplating continuity.

- Compare centre and edge thickness/planarity observations and classify dishing, erosion or incomplete clear.

- Trace how PVD coverage or electroplating voids can change the apparent CMP result.

- Choose two CMP inputs to review: downforce, platen speed, pad condition, slurry chemistry, flow or polish time.

- For each input, state the expected effect on removal rate, selectivity and within-wafer uniformity.

- Add a post-CMP clean and contamination-control check to the integration plan.

- Define metrology at three points: pre-CMP overburden, post-CMP topography and electrical line/via continuity.

- Write a hold/release rule based on planarity plus electrical evidence.

### Acceptance Criteria

[ ] The layer stack and each module's function are correctly labelled.

[ ] The analysis distinguishes deposition/fill causes from polishing causes.

[ ] The release rule uses both physical and electrical evidence.

### Reflection and Evidence

Why can a visually planar surface still fail electrical verification?

Which measurement best distinguishes dishing from incomplete copper clear?

Save the completed evidence with the A04- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

## Activity 5 - Review an STI Integration Flow

| Field | Details |
| --- | --- |
| Goal | Produce the process-flow and challenge analysis used as the foundation for Practical Performance Task 1. |
| Scenario | TechSemicon is introducing shallow trench isolation for an advanced CMOS product. Electrical spread and active-area CD variation appear after integration, and the review board needs a complete process/evidence chain. |
| Alignment | LO2 · A1, A2, A4 |
| Duration | 75 minutes |
| Folder | activities/activity-05-sti-integration-review/ |

### What You Need

STI process cards, worksheet and evidence template

Legacy LOCOS/STI, lithography, etch, CVD and CMP slides

A3 paper or digital flow-diagram tool

### Step-by-Step

- Arrange the STI cards in order: pad oxide, nitride deposition, lithography, trench etch, liner oxidation, trench fill, CMP and nitride strip.

- For each step, write the purpose, key input and outgoing measurable characteristic.

- Add pre-clean and post-CMP clean controls at the correct points.

- Mark the interfaces where active-area CD, trench depth/profile, voiding, dishing/erosion and stress can be introduced.

- Connect each risk to one suitable measurement such as CD-SEM, cross-section SEM/TEM, film thickness, topography or electrical isolation test.

- Compare STI with LOCOS and state why STI supports scaling despite its integration challenges.

- Choose two control points for a pilot-line hold/release plan.

- Draw the final simplified flow without referring to the cards.

- Use the checklist to review completeness, sequence and evidence traceability.

### Acceptance Criteria

[ ] The eight core STI stages are in the correct order and have a purpose.

[ ] At least four implementation challenges are linked to measurements.

[ ] The flow explains both scaling benefit and integration risk.

### Reflection and Evidence

Which STI step most directly controls active-area CD?

How can CMP-induced topography alter a later lithography process window?

Save the completed evidence with the A05- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

## Activity 6 - Analyse Yield and Process Capability

| Field | Details |
| --- | --- |
| Goal | Recreate and improve the legacy ProcessCapability exercise using an auditable Excel workbook with dynamic formulas. |
| Scenario | A gate module has a target CD of 100 nm with specification limits at 90 and 110 nm. The process owner needs Cp/Cpk evidence and a reasoned yield-risk statement before qualification. |
| Alignment | LO2 · K2, A3, A4 |
| Duration | 75 minutes |
| Folder | activities/activity-06-yield-capability-analysis/ |

### What You Need

ProcessCapability.xlsx in this folder

Legacy Cp/Cpk, sigma, yield and defect-density slides

Worksheet and evidence template

### Step-by-Step

- Open ProcessCapability.xlsx and read the Instructions sheet before changing any inputs.

- Go to Data and confirm the 30 hardcoded CD observations are shown in blue text.

- Review the Analysis formulas for mean, sample standard deviation, Cp and Cpk; do not replace formulas with values.

- Compare the mean with the 100 nm target and describe accuracy (centering).

- Compare the standard deviation with the specification width and describe precision (spread).

- Interpret Cp as potential capability and Cpk as actual capability considering centering.

- Change one blue input value to 118 nm and observe how the metrics and out-of-spec count recalculate; then restore the value.

- Use the histogram and capability summary to decide capable, conditionally capable or not capable.

- Record one containment action and one long-term process action.

- Export the Analysis sheet to PDF or capture a screenshot named A06-capability-evidence.

### Acceptance Criteria

[ ] Workbook formulas remain intact and show no Excel errors.

[ ] The learner distinguishes Cp from Cpk and links both to process evidence.

[ ] The decision includes containment, corrective action and verification.

### Reflection and Evidence

Why can Cp be acceptable while Cpk is unacceptable?

Why does a capability index not prove that the process is statistically stable?

Save the completed evidence with the A06- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

## Activity 7 - Respond to an SPC CD Excursion

| Field | Details |
| --- | --- |
| Goal | Recreate the legacy P-chart/SPC exercises and generate the corrective-action chain used in Practical Performance Task 2. |
| Scenario | STI active-area CD is drifting across production lots. A point crosses the upper control limit and a seven-point upward run appears before the alarm. The team must contain risk and restore control. |
| Alignment | LO2 · K2, A3, A4, A5 |
| Duration | 90 minutes |
| Folder | activities/activity-07-spc-cd-excursion/ |

### What You Need

SPCdata.xlsx and p_Chart.xlsx in this folder

Legacy control-limit, Xbar/R, p/c/u-chart and out-of-control rule slides

Corrective-action worksheet and evidence template

### Step-by-Step

- Open SPCdata.xlsx and review the raw subgroup CD data, timestamps, tool IDs and lot IDs.

- Check that subgroup means and ranges use formulas and that the chart updates when a blue input changes.

- Identify the first out-of-control point and the earlier non-random run signal.

- Separate control limits from product specification limits in the worksheet.

- Write the immediate containment actions: stop/hold affected lots, preserve evidence, notify ownership and prevent automatic release.

- Stratify the data by tool/chamber, wafer position, product and time to narrow the source.

- Review lithography focus/dose, etch endpoint/profile and metrology calibration as candidate causes.

- Define confirmation measurements using pre-etch CD, post-etch CD and cross-section profile evidence.

- Select a corrective action and a controlled engineering split; state the rollback trigger.

- Verify recovery using consecutive stable subgroups and an updated capability check.

- Open p_Chart.xlsx and repeat the logic for variable sample sizes using defect proportion rather than CD measurements.

- Export the SPC evidence and complete the follow-up action record.

### Acceptance Criteria

[ ] The response identifies both limit violation and non-random pattern.

[ ] Containment precedes root-cause adjustment and protects affected lots.

[ ] Corrective action, verification criteria and follow-up owner are explicit.

### Reflection and Evidence

Why must the team investigate a non-random run even when all points remain inside control limits?

Which chart is appropriate for CD measurements, and which is appropriate for defect proportions?

Save the completed evidence with the A07- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

## Activity 8 - Run a Future-Technology Integration Gate

| Field | Details |
| --- | --- |
| Goal | Combine the entire course into a structured technology-gate recommendation without treating future devices as isolated marketing concepts. |
| Scenario | A product team is deciding whether to adopt chiplet packaging, FinFET or GAAFET for its next platform. Integration readiness must be assessed using process, performance, reliability and packaging evidence. |
| Alignment | LO2 · K1, K2, A2, A3, A4, A5 |
| Duration | 60 minutes |
| Folder | activities/activity-08-technology-integration-gate/ |

### What You Need

Technology-gate worksheet and evidence template

Legacy packaging, heterogeneous integration, chiplet, FinFET, GAAFET, vertical transistor and 2D-material slides

Outputs from Activities 1-7

### Step-by-Step

- Choose one candidate: chiplet integration, FinFET scaling or GAAFET scaling.

- List the required process modules and identify which existing modules need a new material, geometry, tool or control method.

- Map three critical cross-module interactions and the performance metric each can affect.

- Define device metrics (for example leakage, drive current, resistance or capacitance) and reliability metrics relevant to the candidate.

- Add packaging/interconnect implications, including thermal, mechanical and known-good-die considerations where applicable.

- Create a five-row evidence gate: process capability, metrology readiness, electrical performance, reliability and yield/manufacturability.

- Set a pass/conditional/fail threshold for every gate.

- Identify the largest uncertainty and design the smallest engineering experiment that can reduce it.

- Present a recommendation: proceed, proceed with conditions, or defer.

- Record the next owner, due date and evidence required to close the decision.

### Acceptance Criteria

[ ] The recommendation integrates process, device, reliability, yield and packaging evidence.

[ ] Every gate has a measurable threshold and an accountable follow-up action.

[ ] The conclusion is conditional on evidence rather than technology hype.

### Reflection and Evidence

Which legacy process controls remain useful for the chosen technology?

What new metrology or reliability evidence is essential before volume manufacturing?

Save the completed evidence with the A08- prefix and record the final release/hold/recommendation decision in evidence-template.pdf or evidence-template.md.

# Quick Reference

| Field | Details |
| --- | --- |
| Pattern transfer | Mask/resist -> expose/develop -> inspect CD -> etch -> strip/clean -> verify profile |
| Implant/thermal | Dose/energy/tilt -> implant -> damage/channeling check -> anneal/RTP -> sheet resistance/profile verification |
| Film/CMP | Surface prep -> barrier/seed or film -> fill/deposition -> thickness/profile -> CMP -> clean -> electrical verification |
| SPC response | Contain -> stratify -> confirm -> correct -> verify -> document follow-up |
| Capability | Establish stability first; then compare Cp and Cpk against the approved threshold |
| Evidence | Use the measurement that can distinguish competing causes, not merely the easiest available measurement |

# Assessment Flow

- TRAQOM - scan the digital-attendance QR code on the LMS.

- Complete Assessment Digital Attendance.

- Complete the Written Assessment, then the Practical Performance assessment.

- Upload completed answers on the LMS.

- Sign the Assessment Summary Record.

Courseware and assessment portal: https://lms-tms.tertiaryinfotech.com/

# Support

Email enquiry@tertiaryinfotech.com or call +65 6100 0613. Course page: https://www.tertiarycourses.com.sg/wsq-mastering-semiconductor-key-modules-for-enhanced-cmos-process-integration-and-device-performance.html